Copyright 2019 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

This Product MasterSpec Section is licensed by Deltek, Inc. to VIVA Railings, LLC ("Licensee").

This Product MasterSpec Section modifies the original MasterSpec text and does not include the full content of the original MasterSpec Section.

Revisions made to the original MasterSpec text are made solely by the Licensee and are not endorsed by, or representative of the opinions of, Deltek or The American Institute of Architects (AIA). Neither AIA nor Deltek are liable in any way for such revisions or for the use of this Product MasterSpec Section by any end user. A qualified design professional should review and edit the document to suit Project requirements.

For more information, contact VIVA Railings, LLC, 151 W. Vista Ridge Mall Dr., Lewisville, TX 75067; Phone: (972) 353-8482; Fax: (972) 353-0013; Website: vivarailings.com; Email: info@vivarailings.com.

For information about MasterSpec, contact Deltek at (800) 424-5080 or visit masterspec.com.

SECTION 057300 - DECORATIVE METAL RAILINGS

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Access Product MasterSpec Sections:

<Double click here to view the list of manufacturer Sections available at ProductMasterSpec.com.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

- GENERAL

      - SUMMARY

        - Section Includes:

          - [Stainless steel] [Steel] decorative metal railings[, with infill panels].

          - Illuminated railings.

          - Wood railings.

          - Fasteners.

          - Miscellaneous materials.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 055213 "Pipe and Tube Railings" for nonornamental railings fabricated from pipes and tubes.

          - Section 057313 "Glazed Decorative Metal Railings" for structural glass-supported decorative metal railings and post-supported railings with glass-infill panels.

          - [Section 061000 "Rough Carpentry"] [Section 061053 "Miscellaneous Rough Carpentry"] for wood blocking for anchoring railings.

          - [Section 064013 "Exterior Architectural Woodwork"] [Section 064023 "Interior Architectural Woodwork"] for wood railings.

      - DEFINITIONS

        - Railings: Guards, handrails, and similar devices used for protection of occupants at open-sided floor areas and for pedestrian guidance and support, visual separation, or wall protection.

      - COORDINATION AND SCHEDULING

        - Coordinate installation of anchorages for railings. Furnish setting drawings, templates, and directions for installing anchorages, including sleeves, concrete inserts, anchor bolts, and items with integral anchors, that are to be embedded in concrete or masonry. Deliver items to Project site in time for installation.

        - Schedule installation so wall attachments are made only to completed walls. Do not support railings temporarily by any means that do not meet structural performance requirements.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

      - ACTION SUBMITTALS

        - Product Data:

          - Manufacturer's product lines of [stainless steel] [steel] decorative metal railings assembled from standard components.

          - Stainless steel cable and cable fittings infill.

          - Perforated metal infill panels.

          - Woven-wire mesh infill panels.

          - Horizontal multiline infill panels.

          - Vertical picket infill panels.

          - Cable net infill panels.

          - Illuminated railings.

          - Wood railings.

          - Fasteners.

          - Post-installed anchors.

          - Handrail brackets.

          - Bituminous paint.

          - Nonshrink, nonmetallic grout.

          - Anchoring cement.

          - Metal finishes.

        - Sustainable Design Submittals:

Retain "Product Data" Subparagraph below to require minimum recycled content for LEED v4.1, MRc 4.1 and 4.2 - "Recycled Content."

          - Product Data: For recycled content, indicating postconsumer and preconsumer recycled content and cost.

          - Chain-of-Custody Certificates: For certified wood products. Include statement of costs.

        - Shop Drawings: Include plans, elevations, sections, and attachment details.

          - For illuminated railings, include wiring diagrams and roughing-in details.

Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs below for two-stage Samples.

        - Samples for Initial Selection: For products involving selection of color, texture, or design.

        - Samples for Verification: For each type of exposed finish required.

Delete or revise first three subparagraphs below.

          - Sections of each distinctly different linear railing member, including handrails, top rails, posts, and balusters

          - Illuminated railing.

          - Fittings, end caps, and brackets.

          - Cable and cable hardware and connections.

          - Assembled Sample of railing system, made from full-size components, including top rail, post, [illuminated] handrail, and guard infill. Sample need not be full height.

            - Show method of [connecting] [and] [finishing] members at intersections.

Retain "Delegated Design Calculations" Paragraph below if design services have been delegated to Contractor.

        - Delegated Design Calculations: For railings, including analysis data signed and sealed by the qualified professional engineer responsible for their preparation.

      - INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements" and as may be supplemented in "Quality Assurance" Article.

Testing is by Owner.

        - Qualification Data: For [delegated design professional engineer] [testing agency] [manufacturer-certified Installer].

      - QUALITY ASSURANCE

        - Installer Qualifications: The manufacturer of railing system or a qualified installation firm that is approved, authorized, or licensed by railing system manufacturer to install manufacturer's products.

        - Welding Qualifications: Qualify procedures and personnel in accordance with the following:

Retain applicable subparagraphs below to match railing materials used in Project. Most of VIVA Railings' connections are mechanical, but field welding may be required in some cases.

          - AWS D1.6/D1.6M, "Structural Welding Code - Stainless Steel."

          - AWS D1.1/D1.1M, "Structural Welding Code - Steel."

      - Mockups

        - Build mockups to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for fabrication and installation.

Mockups may be designed as separate decorative elements and left in place.

          - Build mockups as [cut-down assembly] [full-height assembly] [indicated on Drawings].

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - FIELD CONDITIONS

If possible, design railings so they do not have to fit other construction, and delete this article.

        - Field Measurements: Verify actual locations of walls and other construction contiguous with railings by field measurements before fabrication and indicate measurements on Shop Drawings.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - SOURCE LIMITATIONS

        - Obtain decorative metal railing systems from single source from single manufacturer. Systems must be designed, engineered, and fabricated by manufacturer of railing system.

      - MANUFACTURERS

VIVA Railings, LLC, offers a full line of pre-engineered stainless steel or steel post, railing, and guard systems as specified below. For visual overview, see https://vivarailings.com/products/.

Standard VIVA Railings are fabricated using stainless steel or steel pipe, tubing, and plate in the following configurations and profiles and are available with various infill options listed below. Coordinate with VIVA Railings.

        - [Stainless Steel] [Steel] Decorative Metal Railings:

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

          - Basis-of-Design Product: Subject to compliance with requirements, provide VIVA Railings, LLC; BLADE Air Railing System or comparable product by one of the following:

            - <Insert manufacturer's name>.

        - Illuminated Decorative Metal Railings:

VIVA Railings, LLC, offers two options for LED illuminated railings; the "Linear" option, which uses a slotted round rail to house the high-performance LED assembly; and the "Pods" option, which uses a variety of rail and post profiles to house the LED lights at spacing depending upon the amount of illumination desired. See https://vivarailings.com/products/led-illuminated-railing-system/ for additional information.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

          - Basis-of-Design Product: Subject to compliance with requirements, provide VIVA Railings, LLC; iRAIL [Linear] [Pods] Railing System or comparable product by one of the following:

            - <Insert manufacturer's name>.

        - Product Options: Drawings indicate size, profiles, and dimensional requirements of railings and are based on the specific system indicated. See Section 016000 "Product Requirements."

          - Do not modify intended aesthetic effects, as judged solely by Architect, except with Architect's approval. If modifications are proposed, submit comprehensive explanatory data to Architect for review.

      - PERFORMANCE REQUIREMENTS

        - General: For engineering decorative metal railings to withstand structural loads indicated, determine allowable design working stresses of railing materials based on the following:

          - Stainless Steel: 45 percent of minimum yield strength.

          - Steel: 72 percent of minimum yield strength.

        - Structural Performance: Decorative metal railings, including attachment to building construction, shall withstand the effects of gravity loads and the following loads and stresses within limits and under conditions indicated:

Subparagraphs below are based on the International Building Code; revise to suit Project and to comply with requirements of authorities having jurisdiction.

          - Handrails and Top Rails of Guards:

            - Uniform load of 50 lbf/ft. (0.73 kN/m) applied in any direction.

            - Concentrated load of 200 lbf (0.89 kN) applied in any direction.

            - Uniform and concentrated loads need not be assumed to act concurrently.

          - Infill of Guards:

            - Concentrated load of 50 lbf (0.22 kN) applied horizontally on an area of 1 sq. ft. (0.093 sq. m).

            - Infill load and other loads need not be assumed to act concurrently.

Delete "Thermal Movements" Paragraph below if only interior railings are required.

        - Thermal Movements: Allow for thermal movements from ambient and surface temperature changes acting on exterior railings by preventing buckling, opening of joints, overstressing of components, failure of connections, and other detrimental effects.

Differential values in "Temperature Change" Subparagraph below are suitable for most of the United States.

          - Temperature Change: 120 deg F (67 deg C), ambient; 180 deg F (100 deg C), material surfaces.

      - METALS, GENERAL

        - Metal Surfaces, General: Provide materials with smooth surfaces, without seam marks, roller marks, rolled trade names, stains, discolorations, or blemishes.

        - Brackets, Flanges, and Anchors: Same metal and finish as supported rails unless otherwise indicated.

          - Provide stainless steel wall brackets with flange tapped for concealed anchorage with vertical and horizontal adjustment capability.

      - [STAINLESS STEEL] [STEEL] DECORATIVE METAL RAILINGS

Retain "Recycled Content of Stainless Steel Products" Paragraph below to specify recycled content if required. An alternative method of requiring recycled content is to retain requirement in Project's Division 01 sustainable design requirements Section that gives Contractor the option and responsibility to determine how recycled content requirements will be met.

        - Recycled Content of Stainless Steel Products: Postconsumer recycled content plus one-half of preconsumer recycled content not less than 65 percent.

VIVA Railings' stainless steel standards are Types 304 and 316. Type 316L is available upon special request and with additional cost for use on projects requiring better resistance to corrosion and exposure to de-icing salts. Coordinate material options with VIVA Railings.

Retain material types, qualities, and grades in this article that are indicated in the Specifications or on Drawings. Grade designations MT, TP, and CF below relate to the form of metal (tubing, pipe, or castings) being specified.

Primary difference between round stainless steel tubing and stainless steel pipe is in outside dimensions. Pipe sizes are normally indicated by using nominal pipe size designator and weight class or schedule number; for tubing, OD, and wall thickness are used.

        - Stainless Steel Tubing: ASTM A554, [Grade MT 304] [Grade MT 316].

        - Stainless Steel Pipe: ASTM A312/A312M, [Grade TP 304] [Grade TP 316].

Retain first option in "Castings" Paragraph below with Type 304; retain second option with Type 316.

        - Stainless Steel Castings: ASTM A743/A743M, [Grade CF 8 or CF 20] [Grade CF 8M or CF 3M].

        - Stainless Steel Sheet, Strip, Plate, and Flat Bar: ASTM A666, [Type 304] [Type 316].

        - Stainless Steel Bars and Shapes: ASTM A276, [Type 304] [Type 316].

        - Steel Bars: Hot-rolled, carbon steel complying with ASTM A29/A29M, Grade 1010.

Standard posts for cantilevered structural post railings and guards specified in this article are fabricated from stainless steel plate, tubing, and bars in the following configurations and profiles and are available with various infill options as listed below:

BLADE Air: Top-, fascia-, or core-mounted to steel stringer or balcony slab edge with 2-inch- (50-mm-) deep parallel double-plate posts (wire mesh, perforated metal, horizontal multiline, vertical picket, and cable net infills); see https://vivarailings.com/products/blade-air-wire-mesh-railing-system for product options.

        - Posts: Parallel double plate, made from [stainless steel] [steel].

Top rails are available in 1-1/2- or 2-inch-diameter round and 2 by 1 inch rectangular tubular stainless steel shapes and 2-inch-diameter round wood shapes.

        - Top Rail/Hand Rail: [Tubular stainless steel pipe] [Wood] [Illuminated] with [round] [rectangular] cross-section shape.

Standard woven-wire-mesh infill panel material is stainless steel. Aluminum, brass, bronze, copper, and copper alloys are available options.

Product options include custom fabrications using aluminum or steel posts with various finishes, in lieu of stainless steel. Coordinate with VIVA Railings.

Retain "Stainless Steel Cable and Cable Fitting Infill" Paragraph below if cable is used as railing infill. The terms "cable" and "wire rope" are both used; revise to "wire rope" if preferred. "Cable" is used here, because "wire rope" usually refers to diameters of larger than 3/8 inch (9.5 mm), VIVA Railings and most other manufacturers use the term "cable."

Cable infill designs specified below are available with VIVA Railings' BEACON Railing System.

        - Stainless Steel Cable and Cable Fitting Infill:

          - Cable: 1-by-19 wire cable made from wire complying with ASTM A492, Type 316.

          - Cable Diameter: 3/16 inch (5 mm).

          - Cable Fittings: Swageless hardware fabricated from stainless steel, with capability to sustain, without failure, a load equal to minimum breaking strength of cable with which they are used.

Perforated metal infill panels are available with VIVA Railings' BLADE Air Railing System. See https://vivarailings.com/infill-systems-guide/perforated-metal-panel-infill/ for perforation pattern options.

        - Perforated Metal Infill Panels: Stainless steel sheet with perforations, ASTM A240/A 240M or ASTM A666, [Type 304] [Type 316L], manufacturer's standard thickness, within nominal 1-inch- (25-mm-) wide by 9/16-inch- (15-mm-) deep fully-welded stainless steel "C-shaped" frame, ground smooth without visible seams.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product.

          - Basis-of-Design Product: Subject to compliance with requirements, provide VIVA Railings, LLC; [PMRO-0610] [PMRO-1014] [PMRO-1217] [PMSL-0325] [PMSL-1122] [PMSQ-1013].

Woven-wire mesh infill panels are available with VIVA Railings' BLADE Air Railing System. Maximum panel width is 5 ft. (1.219 m). See https://vivarailings.com/infill-systems-guide/wire-mesh-infill/ for woven-wire mesh pattern options.

        - Woven-Wire Mesh Infill: Intermediate-crimp, woven-wire or woven-strap mesh, made from wire complying with ASTM A580/A580M, [Type 304] [Type 316], in a 0.98-inch- (25-mm-) wide by 0.59-inch- (15-mm-) deep fully-welded stainless steel "C" frame, ground smooth without visible seams.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product.

          - Basis-of-Design Product: Subject to compliance with requirements, provide VIVA Railings, LLC; WM-[10] [11] [12] [13] [14] [15] [17] [19] [20] [21].

Horizontal multiline infill panels can be used in VIVA Railings' BLADE Air Railing System.

        - Horizontal Multiline Infill Panels: 1/2-inch (38-mm) round stainless steel tubing rods.

Vertical picket infill panels can be used in VIVA Railings' BLADE Air Railing System.

        - Vertical Picket Infill Panels: 1/2-inch (38-mm) round stainless steel pickets.

Retain "Cable Net Infill" Paragraph below if "CableNet" is used as railing infill. Cable net infill specified below is available with VIVA Railings' BEACON Railing System.

        - Cable Net Infill Panels: 1/16 inch (1.5 mm) stainless steel cable mesh with 1 inch (102 mm) wide frame.

      - ILLUMINATED RAILINGS

Revise "General" Paragraph below if using another type of railing. Product below is VIVA Railings' standard. See https://vivarailings.com/products/led-illuminated-railing-system/ for product options.

VIVA Railings iRAIL can be used as a Top Rail, Glass Top Cap, Assist Rail, Wall Rail, or FSR application.

        - General: Comply with requirements in this Section for metal railings with welded connections.

        - Illuminated Units: Provide internally wired [1-1/2-inch- (38-mm-) diameter stainless steel] [2-inch- (51-mm-) diameter stainless steel] [2-inch- (50-mm-) diameter wood] rail with integral LED light fixture system to illuminate walking surfaces adjacent to railings without light leaks. Make provisions for servicing and for concealed connection to electric service. Coordinate electrical characteristics with power supply provided.

          - Light Color: [Cool white; 4000 K] [Warm white; 3000 K].

          - IP Rating: IP67.

Retain next six subparagraphs below for iRail Linear illuminated rail system.

          - Light Output: [185 lumens/ft.] [250 lumens/ft.]

          - Beam Angle: 120 degrees.

          - Orientation: [Symmetrical] [Asymmetrical at 30 degrees].

          - LED Lens: [Clear] [Frosted].

          - CRI: Less than 90.

          - Power Supply: [120 V] [277 V] ac input, 12 V dc output.

Retain next six subparagraphs below for iRail Pods illuminated rail system.

          - Light Spacing: [18 inches (457 mm)] [36 inches (914 mm)] o.c.

          - Light Output: [90 lumens] [76 lumens].

          - Beam Angle: 60 degrees.

          - Orientation: [Symmetrical] [Asymmetrical at 22 degrees].

          - CRI: Less than 90.

          - Power Supply: [120 V] [277 V] ac input, 24 V dc output.

      - WOOD RAILINGS

Retain one of two "Description" paragraphs below. Retain first paragraph if wood rails are supplied by railing manufacturer; retain second paragraph if they are supplied by architectural woodworker in Division 06.

        - Description: Clear, straight-grained hardwood rails secured to [recessed] [exposed] metal substrate.

Other species in "Species" Subparagraph below are available upon request from VIVA Railings. All VIVA Railings' wood rails are shipped unfinished for field finishing under Section 099123 "Interior Painting." Standard shape and size is round, 2-inch (50-mm) diameter.

          - Species: [Cherry] [Maple] [Red oak] [White oak] <Insert species>.

          - Finish: Manufacturer's standard unfinished.

          - Staining: In accordance with Section 099123 "Interior Painting."

If rails are required to serve as handrails rather than only as top rails of guards, verify that profile specified will comply with applicable regulations for accessibility to people with disabilities.

          - Top Rail Profile: [Square, 1-3/4 by 1-3/4 inches (45 by 45 mm) with edges eased to 1/4-inch (6-mm) radius] [Rectangular, 1-3/4 by 5 inches (45 by 127 mm) with edges eased to 1/4-inch (6-mm) radius] [Round, 2-inch (50-mm) diameter] [As indicated] <Insert description>.

          - Handrail Profile: [Round, 2-inch (50-mm) diameter] [Round, 1-1/2-inch (38 mm) diameter, reinforced] [Rectangular, 1-1/4 by 1-3/4 inches (32 by 45 mm) with edges eased to 1/4-inch (6-mm) radius] [As indicated] <Insert description>.

First "Certified Wood" Subparagraph below applies to LEED 2009 and LEED v4. Manufacturers certifying products as "FSC Mixed Credit" do not have to use 100 percent certified wood in the products; however, in their total production, manufacturers must use an amount equal to or greater than the percentage of their production that is labeled "FSC Mixed Credit."

          - Certified Wood: Wood products shall be certified as "FSC Pure"[ or "FSC Mixed Credit"] in accordance with FSC STD-01-001 and FSC STD-40-004.

"Certified Wood" Subparagraph below applies to IgCC.

          - Certified Wood: Wood products shall be labeled in accordance with the AF&PA's Sustainable Forestry Initiative, be certified as "FSC Pure" in accordance with FSC STD-01-001 and FSC STD-40-004, or be certified and labeled in accordance with the standards of the Programme for Endorsement of Forest Certification.

"Certified Wood" Subparagraph below applies to ASHRAE 189.1.

          - Certified Wood: Wood products shall [contain not less than 60 percent] [be made from] certified wood tracked through a chain-of-custody process. Certified wood documentation shall be provided by sources certified through a forest certification system with principles, criteria, and standards developed using ISO/IEC Guide 59 or the World Trade Organization's "WTO Agreement on Technical Barriers to Trade."

"Certified Wood" Subparagraph below applies to Green Globes.

          - Certified Wood: Wood products shall be certified in accordance with the American Tree Farm System's "AFF Standard," the AF&PA's Sustainable Forestry Initiative, FSC STD-01-001 and FSC STD-40-004, or the standards of the Programme for Endorsement of Forest Certification.

        - Description: Hardwood rails complying with Section 064023 "Interior Architectural Woodwork."

      - FASTENERS

        - Fastener Materials: Unless otherwise indicated, provide the following:

Retain or revise applicable requirements in subparagraphs below.

          - For [Stainless Steel] [and] [Steel] Railing Components: [Type 304] [Type 316] stainless steel fasteners.

          - For Dissimilar Metal Railing Components: [Type 304] [Type 316] stainless steel fasteners.

Retain subparagraph below if exposed fasteners are allowed, especially with color anodic finish.

          - Finish exposed fasteners to match appearance, including color and texture, of railings.

        - Fasteners for Anchoring to Other Construction: Select fasteners of type, grade, and class required to produce connections suitable for anchoring railings to other types of construction[ and capable of withstanding design loads].

        - Provide concealed fasteners for interconnecting railing components and for attaching railings to other work unless [otherwise indicated] [exposed fasteners are unavoidable] [exposed fasteners are the standard fastening method for railings indicated].

Revise subparagraph below if another type of head is required or is standard with system specified.

          - Provide hex, hex socket, or hex-button head machine screws for exposed fasteners unless otherwise indicated.

In "Post-Installed Anchors" Paragraph below, ICC-ES AC193 is for mechanical anchors, and ICC-ES AC308 is for adhesive anchors.

        - Post-Installed Anchors: Fastener systems with working capacity greater than or equal to the design load, in accordance with an evaluation report acceptable to authorities having jurisdiction, based on ICC-ES AC193[ or ICC-ES AC308].

Material in "Material for Interior Locations" Subparagraph below protects against corrosion in an indoor atmosphere.

          - Material for Interior Locations: Carbon-steel components zinc plated to comply with ASTM B633 or ASTM F1941/F1941M, Class Fe/Zn 5, unless otherwise indicated.

First option in "Material for Exterior Locations and Where Stainless Steel Is Indicated" Subparagraph below refers to Type 304 and similar alloys; second option refers to Type 316 and similar alloys.

          - Material for Exterior Locations and Where Stainless Steel Is Indicated: Alloy [Group 1 (A1)] [Group 2 (A4)] stainless steel bolts, ASTM F593 and nuts, ASTM F594.

      - MISCELLANEOUS MATERIALS

        - Handrail Brackets: Stainless steel with center of handrail [2-1/2 inches (63.5 mm)] [3-1/8 inches (79.4 mm)] <Insert dimension> from [face of railing] [wall].

Usually retain one of three subparagraphs below that corresponds with type of bracket used. Delete all three if wall rails are not used.

          - Provide brackets with flange tapped for concealed anchorage to threaded hanger bolt.

          - Provide brackets with predrilled hole for exposed bolt anchorage.

          - Provide brackets with predrilled hole for bolted anchorage and with snap-on cover that matches rail finish and conceals bracket base and bolt head.

Retain "Welding Rods and Bare Electrodes" Paragraph below to suit Project.

        - Welding Rods and Bare Electrodes: Select in accordance with AWS specifications for metal alloy welded.

          - Provide type and alloy as recommended by producer of metal to be welded and as required for color match, strength, and compatibility in fabricated items.

        - Bituminous Paint: Cold-applied asphalt emulsion complying with ASTM D1187/D1187M.

Retain "Nonshrink, Nonmetallic Grout" or "Anchoring Cement" Paragraph below, or both, to suit Project.

        - Nonshrink, Nonmetallic Grout: Factory-packaged, nonstaining, noncorrosive, nongaseous grout complying with ASTM C1107/C1107M. Provide grout specifically recommended by manufacturer for [interior] [and] [exterior] applications.

        - Anchoring Cement: Factory-packaged, nonshrink, nonstaining, hydraulic-controlled expansion cement formulation for mixing with water at Project site to create pourable anchoring, patching, and grouting compound.

          - Water-Resistant Product: [At exterior locations] [and] [where indicated on Drawings], provide formulation that is recommended in writing to be resistant to erosion from water exposure without needing protection by a sealer or waterproof coating.

      - FABRICATION

        - General: Fabricate decorative metal railings to comply with requirements indicated for design, dimensions, member sizes and spacing, details, finish, and anchorage[, but not less than that required to support structural loads].

        - Shop assemble railings and guards to greatest extent possible to minimize field splicing and assembly. Disassemble units only as necessary for shipping and handling limitations.

          - Clearly mark units for reassembly and coordinated installation.

          - Use connections that maintain structural value of joined pieces.

        - Cut, drill, and punch metals cleanly and accurately.

          - Remove burrs and ease edges to a radius of approximately 1/32 inch (1 mm) unless otherwise indicated.

          - Remove sharp or rough areas on exposed surfaces.

        - Form work true to line and level with accurate angles and surfaces.

        - Fabricate connections that will be exposed to weather in a manner to exclude water.

          - Provide weep holes where water may accumulate.

          - Locate weep holes in inconspicuous locations.

        - Cut, reinforce, drill, and tap as indicated to receive finish hardware, screws, and similar items.

        - Connections: Fabricate railings with [welded] [or] [mechanical] connections unless otherwise indicated.

Delete "Welded Connections" Paragraph below if only mechanical connections are acceptable or are compatible with metals and finishes retained. Connections below are generally applicable to exposed welding of steel and stainless steel.

        - Welded Connections: Cope components at connections to provide close fit, or use fittings designed for this purpose. Weld all around at connections, including at fittings.

          - Use materials and methods that minimize distortion and develop strength and corrosion resistance of base metals.

          - Obtain fusion without undercut or overlap.

          - Remove flux immediately.

          - At exposed connections, finish exposed welds to comply with NOMMA's "Voluntary Joint Finish Standards" for Finish #1 welds; ornamental quality with no evidence of a welded joint.

        - Mechanical Connections: Connect members with concealed mechanical fasteners and fittings.

          - Fabricate members and fittings to produce flush, smooth, rigid, hairline joints.

          - Fabricate splice joints for field connection using an epoxy structural adhesive if this is manufacturer's standard splicing method.

        - Form changes in direction as follows:

Retain one of five subparagraphs below. Second subparagraph allows fabricator to choose radius of bends. Third is for flush (zero-radius) bends. Fourth is for radii that are indicated on Drawings.

          - As detailed.

          - [By bending] [or] [by inserting prefabricated elbow fittings].

          - [By flush bends] [or] [by inserting prefabricated flush-elbow fittings].

          - [By radius bends of radius indicated] [or] [by inserting prefabricated elbow fittings of radius indicated].

          - By bending to smallest radius that will not result in distortion of railing member.

Retain first paragraph below if bending is allowed or required.

        - Bend members in jigs to produce uniform curvature for each configuration required. Maintain cross section of member throughout entire bend without buckling, twisting, cracking, or otherwise deforming exposed surfaces of components.

        - Close exposed ends of hollow railing members with prefabricated cap and end fittings of same metal and finish as railings.

        - Provide wall returns at ends of wall-mounted handrails unless otherwise indicated. Close ends of returns, unless clearance between end of rail and wall is 1/4 inch (6 mm) or less.

        - Brackets, Flanges, Fittings, and Anchors: Provide wall brackets, flanges, handrail brackets, miscellaneous fittings, and anchors to interconnect railing members to other Work unless otherwise indicated.

Retain subparagraph below if any railings are supported from plaster or gypsum board walls.

          - At brackets and fittings fastened to plaster or gypsum board partitions, provide crush-resistant fillers or other means to transfer loads through wall finishes to structural supports and to prevent bracket or fitting rotation and crushing of substrate.

        - Provide inserts and other anchorage devices for connecting railings to concrete or masonry Work.

          - Fabricate anchorage devices capable of withstanding loads imposed by railings.

          - Coordinate anchorage devices with supporting structure.

Delete first paragraph below if no posts are set in concrete or if posts are set without sleeves.

        - For railing posts set in concrete, provide stainless steel sleeves not less than 6 inches (150 mm) long with inside dimensions not less than 1/2 inch (13 mm) greater than outside dimensions of post, with metal plate forming bottom closure.

Retain first paragraph below if required or if allowed by authorities having jurisdiction.

        - For removable railing posts, fabricate slip-fit sockets from stainless steel tube or pipe whose ID is sized for a close fit with posts; limit movement of post without lateral load, measured at top, to not more than one-fortieth of post height.

          - Provide socket covers designed and fabricated to resist being dislodged.

          - Provide chain with eye, snap hook, and staple across gaps formed by removable railing sections at locations indicated. Fabricate from same metal as railings.

        - Stainless Steel Cable Guard Infill: Fabricate cable guard infill assemblies in the shop to field-measured dimensions with fittings machine swaged.

          - Minimize amount of turnbuckle take-up used for dimensional adjustment, so maximum amount is available for tensioning cable.

          - Tag cable assemblies and fittings to identify installation locations and orientations for coordinated installation.

        - Perforated-Metal Infill Panels: Fabricate infill panels from perforated metal made from [aluminum] [stainless steel] [same metal as railings in which they are installed].

          - Frame panels with C-shaped channels made from stainless steel sheet, not less than 0.043 inch (1.1 mm) thick.

          - Orient perforated metal with pattern parallel to ground.

        - Woven-Wire Mesh Infill Panels: Fabricate infill panels from woven-wire mesh crimped into 1-by-1/2-by-1/8-inch (25-by-13-by-3-mm) metal channel frames.

          - Fabricate woven-wire mesh and frames from [aluminum] [stainless steel] [steel] [bronze] [brass] [copper] [unless otherwise indicated].

          - Orient woven-wire mesh with [diamonds vertical] [wires perpendicular and parallel to top rail] [wires horizontal and vertical].

Retain "Toe Boards" Paragraph below if required for protection against objects falling over edge on to trafficked surfaces.

        - Toe Boards: Where indicated on Drawings, provide toe boards at railings around openings and at edge of open-sided floors and platforms. Fabricate to dimensions and details indicated.

      - METAL FINISH REQUIREMENTS, GENERAL

        - Comply with NAAMM's "Metal Finishes Manual for Architectural and Metal Products" recommendations for applying and designating finishes.

        - Protect mechanical finishes on exposed surfaces from damage by applying a strippable, temporary protective covering before shipment.

Retain "Appearance of Finished Work" Paragraph below for variable finishes, such as anodized or patina finishes.

        - Appearance of Finished Work: Noticeable variations in same piece are unacceptable. Variations in appearance of abutting or adjacent pieces are acceptable if they are within one-half of the range of approved Samples. Variations in appearance of other components are acceptable if they are within the range of approved Samples and are assembled or installed to minimize contrast.

Retain paragraph below if exposed fasteners are allowed, especially with color anodic finish.

        - Provide exposed fasteners with finish matching appearance, including color and texture, of railings.

      - STAINLESS STEEL FINISHES

        - Surface Preparation: Remove tool and die marks and stretch lines, or blend into finish.

        - Stainless Steel Finishes:

Retain "Color Electro-Plated Metal" Subparagraph to suit Project.

          - Color Electro-Plated Metal: Vertical and stand-off components.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

Finish in "Dull Satin Finish" Subparagraph below is a nondirectional finish produced from a No. 4 finish by brushing with a 380-grit extremely fine abrasive to remove the grit lines without producing a reflective appearance.

          - Dull Satin Finish: ASTM A480/A480M, No. 6.

Retain option in paragraph below for exterior rails.

        - When polishing is completed,[ passivate and] rinse surfaces. Remove embedded foreign matter and leave surfaces chemically clean.

      - STEEL FINISHES

        - Surface Preparation: Remove tool and die marks and stretch lines, or blend into finish.

        - Powder-Coat Finish: AAMA 2603 except with a minimum dry film thickness of 1.5 mils (0.04 mm). Comply with coating manufacturer's written instructions for cleaning, conversion coating, and applying and baking finish.

          - Color and Gloss: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color and gloss>.

- EXECUTION

      - EXAMINATION

Delete first paragraph below if no handrails are attached to plaster or gypsum board assemblies.

        - Examine plaster and gypsum board assemblies, where reinforced to receive anchors, to verify that locations of concealed reinforcements have been clearly marked for Installer. Locate reinforcements and mark locations if not already done.

        - Installation Tolerances: Structural steel and concrete slabs to be within 1/8 inch (3 mm) in 10 ft. (3.048 m) horizontally and 1/8 inch (3 mm) vertically. Correct out-of-tolerance conditions to meet railing manufacturer's requirements.

      - INSTALLATION, GENERAL

        - Perform cutting, drilling, and fitting required for installing railings.

          - Fit exposed connections together to form tight, hairline joints.

          - Install railings level, plumb, square, true to line; without distortion, warp, or rack.

          - Set railings accurately in location, alignment, and elevation; measured from established lines and levels.

          - Do not weld, cut, or abrade surfaces of railing components that have been coated or finished after fabrication and that are intended for field connection by mechanical or other means without further cutting or fitting.

Revise two subparagraphs below if closer tolerances are required. Both are from NAAMM's "Pipe Railing Systems Manual."

          - Set posts plumb within a tolerance of 1/16 inch in 3 ft. (2 mm in 1 m).

          - Align rails so variations from level for horizontal members and variations from parallel with rake of steps and ramps for sloping members do not exceed 1/4 inch in 12 ft. (6 mm in 3 m).

        - Control of Corrosion: Prevent galvanic action and other forms of corrosion by insulating metals and other materials from direct contact with incompatible materials.

        - Adjust railings before anchoring to ensure matching alignment at abutting joints.

        - Fastening to In-Place Construction: Use anchorage devices and fasteners where necessary for securing railings and for properly transferring loads to in-place construction.

      - METAL RAILING CONNECTIONS

Retain "Nonwelded Connections" or "Welded Connections" Paragraph below unless both methods are required. If both mechanical and welded connections are required, indicate locations of each on Drawings.

        - Nonwelded Connections: Use mechanical or adhesive joints for permanently connecting railing components. Use wood blocks and padding to prevent damage to railing members and fittings. Seal recessed holes of exposed locking screws, using plastic cement filler colored to match finish of railings.

        - Welded Connections: Use fully welded joints for permanently connecting railing components. Comply with requirements for welded connections in "Fabrication" Article, whether welding is performed in the shop or in the field.

Retain "Expansion Joints" Paragraph below if expansion joints are required or revise to suit Project. Indicate locations on Drawings based on temperature changes expected and coefficient of expansion of metals involved.

        - Expansion Joints: Install expansion joints at locations indicated but not farther apart than required to accommodate thermal movement. Provide slip-joint internal sleeve, extending 2 inches (50 mm) beyond joint on either side; fasten internal sleeve securely to one side; and locate joint within 6 inches (150 mm) of post.

      - ANCHORING METAL POSTS

Retain type(s) of anchorage in this article to suit Project.

Retain one of first two paragraphs below or delete both if not using posts in concrete. Coordinate with products retained in Part 2.

        - Use stainless steel pipe sleeves preset and anchored into concrete for installing posts. After posts have been inserted into sleeves, fill annular space between post and sleeve with [nonshrink, nonmetallic grout] [or] [anchoring cement], mixed and placed to comply with anchoring material manufacturer's written instructions.

        - Form or core-drill holes in accordance with engineering requirements for installing posts in concrete. Clean holes of loose material, insert posts, and fill annular space between post and concrete with [nonshrink, nonmetallic grout] [or] [anchoring cement], mixed and placed to comply with anchoring material manufacturer's written instructions.

Retain one of first two paragraphs below if retaining either concrete anchorage method.

        - Cover anchorage joint with flange of same metal as post, [welded to post after placing anchoring material] [attached to post with setscrews].

        - Leave anchorage joint exposed with [1/8-inch (3-mm) buildup, sloped away from post] [anchoring material flush with adjacent surface].

Revise first paragraph below if posts are welded directly to supports.

        - Anchor posts to metal surfaces with flanges, angle type, or floor type as required by conditions, connected to posts and to metal supporting members as follows:

          - For [stainless steel] [steel] railings, weld flanges to posts and bolt to metal-supporting surfaces.

Retain paragraph below if applicable.

        - Install removable railing sections, where indicated, in slip-fit metal sockets cast in concrete.

      - ATTACHING RAILINGS

Delete first two paragraphs below if railing ends are not returned to walls.

        - Anchor railing ends to concrete and masonry with [sleeves concealed within] [flanges connected to] [brackets on underside of rails connected to] railing ends and anchored to wall construction with anchors and bolts.

        - Anchor railing ends to metal surfaces with flanges bolted to metal surfaces and [welded to railing ends] [or] [connected to railing ends, using nonwelded connections].

        - Attach handrails to walls with wall brackets[, except where end flanges are used]. Provide brackets with [1-1/2-inch (38-mm)] <Insert dimension> clearance from inside face of handrail and finished wall surface.

          - Use type of bracket with [flange tapped for concealed anchorage to threaded hanger bolt] [predrilled hole for exposed bolt anchorage].

          - Locate brackets as indicated or, if not indicated, at spacing required to support structural loads.

        - Secure wall brackets[ and railing end flanges] to building construction as follows:

          - For concrete and solid masonry anchorage, use drilled-in expansion shields and hanger or lag bolts.

          - For hollow masonry anchorage, use toggle bolts.

          - For wood stud partitions, use hanger or lag bolts set into studs or wood backing between studs. Coordinate with carpentry work to locate backing members.

Retain one of three subparagraphs below if using steel studs.

          - For steel-framed partitions, use hanger or lag bolts set into[ fire-retardant-treated] wood backing between studs. Coordinate with stud installation to locate backing members.

          - For steel-framed partitions, fasten brackets directly to steel framing or concealed steel reinforcements using self-tapping screws of size and type required to support structural loads.

          - For steel-framed partitions, fasten brackets with toggle bolts installed through flanges of steel framing or through concealed steel reinforcements.

      - FIELD QUALITY CONTROL

Retain this article if field testing for compliance with performance requirements is required.

        - Testing Agency: Owner will engage a qualified testing agency to perform tests and inspections and to prepare test reports. Payment for these services will be made [by Owner] [from the testing and inspecting allowance, as authorized by Change Orders].

Revise "Extent and Testing Methodology" Paragraph below if more extensive testing is required.

        - Extent and Testing Methodology: Testing agency will randomly select completed railing assemblies for testing that are representative of different railing designs and conditions in the completed Work. Test railings in accordance with ASTM E894 and ASTM E935 for compliance with performance requirements.

        - Remove and replace railings where test results indicate that they do not comply with specified requirements unless they can be repaired in a manner satisfactory to Architect and comply with specified requirements.

        - Perform additional testing and inspecting, at Contractor's expense, to determine compliance of replaced or additional work with specified requirements.

      - CLEANING

        - Clean [stainless steel] [and] [steel] by washing thoroughly with clean water and soap, rinsing with clean water, and wiping dry.

        - Clean wood rails by wiping with a damp cloth and then wiping dry.

      - PROTECTION

Maintain railing system with monthly washing with soap and water. This is particularly critical in salt environments or conditions to prevent corrosion.

        - Protect finishes of railings from damage during construction period with temporary protective coverings approved by railing manufacturer. Remove protective coverings at time of Substantial Completion.

        - Restore finishes damaged during installation and construction period, so no evidence remains of correction work. Return items that cannot be refinished in the field to the shop; make required alterations and refinish entire unit, or provide new units.

END OF SECTION 057300