Copyright 2018 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

This Product MasterSpec Section is licensed by Deltek, Inc. to VIVA Railings, LLC ("Licensee").

This Product MasterSpec Section modifies the original MasterSpec text and does not include the full content of the original MasterSpec Section.

Revisions made to the original MasterSpec text are made solely by the Licensee and are not endorsed by, or representative of the opinions of, Deltek or The American Institute of Architects (AIA). Neither AIA nor Deltek are liable in any way for such revisions or for the use of this Product MasterSpec Section by any end user. A qualified design professional should review and edit the document to suit Project requirements.

For more information, contact VIVA Railings, LLC, 151 W. Vista Ridge Mall Dr., Lewisville, TX 75067; Phone: (972) 353-8482; Fax: (972) 353-0013; Website: vivarailings.com; Email: info@vivarailings.com.

For information about MasterSpec, contact Deltek at (800) 424-5080 or visit masterspec.com.

SECTION 057313 - GLAZED DECORATIVE METAL RAILINGS

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on MasterWorks/Single-File Formatting/Toggle/Editor's Notes.

To read detailed research, technical information about products and materials, and coordination checklists, click on MasterWorks/Supporting Information.

Access Product MasterSpec Sections:

<Double click here to view the list of manufacturer Sections available at ProductMasterSpec.com.>

Revise this Section by deleting and inserting text to meet Project-specific requirements.

- GENERAL

      - SUMMARY

        - Section Includes:

          - Exterior post-supported railing and guard systems with glass infill panels.

          - Interior post-supported railing and guard systems with glass infill panels.

          - Illuminated railings.

          - Wood railings.

          - Fasteners.

          - Miscellaneous materials.

        - Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

          - Section 057300 "Decorative Metal Railings" for decorative metal railing and guard systems with non-glass-infill panels.

          - [Section 061000 "Rough Carpentry"] [Section 061053 "Miscellaneous Rough Carpentry"] for wood blocking for anchoring railings.

          - [Section 064013 "Exterior Architectural Woodwork"] [Section 064023 "Interior Architectural Woodwork"] for wood railings.

      - DEFINITIONS

        - Railings: Guards, handrails, and similar devices used for protection of occupants at open-sided floor and exterior deck areas and for pedestrian guidance and support, visual separation, or wall protection.

      - COORDINATION AND SCHEDULING

        - Coordinate installation of anchorages for railings. Furnish setting drawings, templates, and directions for installing anchorages, including sleeves, concrete inserts, anchor bolts, and items with integral anchors, that are to be embedded in concrete or masonry. Deliver items to Project site in time for installation.

        - Schedule installation so wall attachments are made only to completed walls. Do not support railings temporarily by any means that do not meet structural performance requirements.

      - PREINSTALLATION MEETINGS

Retain "Preinstallation Conference" Paragraph below if Work of this Section is extensive or complex enough to justify a conference.

        - Preinstallation Conference: Conduct conference at [Project site] <Insert location>.

If needed, insert list of conference participants not mentioned in Section 013100 "Project Management and Coordination."

      - ACTION SUBMITTALS

        - Product Data:

          - Manufacturer's product lines of glazed decorative metal railings assembled from standard components.

          - Glass products.

          - Illuminated railings.

          - Wood railings.

          - Fasteners.

          - Post-installed anchors

          - Handrail brackets.

          - Nonshrink, nonmetallic grout.

          - Anchoring cement.

          - Metal finishes.

        - Sustainable Design Submittals:

Retain "Product Data" Subparagraph below to require minimum recycled content for LEED v4.1, MRc 4.1 and 4.2 - "Recycled Content."

          - Product Data: For recycled content, indicating postconsumer and preconsumer recycled content and cost.

          - Chain-of-Custody Certificates: For certified wood products. Include statement of costs.

        - Shop Drawings: Include plans, elevations, sections, and attachment details.

          - For illuminated railings, include wiring diagrams and roughing-in details.

Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs below for two-stage Samples.

        - Samples for Initial Selection: For products involving selection of color, texture, or design.

        - Samples for Verification: For each type of exposed finish required.

Delete or revise subparagraphs below.

          - Sections of each distinctly different linear railing member, including handrails, top rails, posts, and balusters.

          - Each type of glass and glass edge required.

          - Illuminated railing.

          - Fittings, end caps, and brackets.

          - Assembled Sample of railing systems, made from full-size components, including [top rail], post, [illuminated] handrail, and glass infill panels. Show method of finishing members at intersections. Sample need not be full height.

Retain "Delegated Design Calculations" Paragraph below if design services have been delegated to Contractor.

        - Delegated Design Calculations: For railings, including analysis data signed and sealed by the qualified professional engineer responsible for their preparation.

      - INFORMATIONAL SUBMITTALS

Coordinate "Qualification Data" Paragraph below with qualification requirements in Section 014000 "Quality Requirements." and as may be supplemented in "Quality Assurance" Article.

Testing Is by Owner.

        - Qualification Data: For [delegated design professional engineer] [testing agency] [manufacturer-certified Installer].

      - QUALITY ASSURANCE

        - Installer Qualifications: The manufacturer of railing system or a qualified installation firm that is approved, authorized, or licensed by railing system manufacturer to install manufacturer's products.

Retain "Welding Qualifications" Paragraph below if shop or field welding is required.

        - Welding Qualifications: Qualify procedures and personnel in accordance with the following:

Retain applicable subparagraphs below to match railing materials used in Project. Most of VIVA Railings' connections are mechanical, but field welding may be required in some cases.

          - AWS D1.6/D1.6M, "Structural Welding Code - Stainless Steel."

          - AWS D1.1/D1.1M, "Structural Welding Code - Steel."

      - Mockups

        - Build mockups to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for fabrication and installation.

Mockups may be designed as separate decorative elements and left in place if approved by Architect.

          - Build mockups as [cut-down assembly] [full-height assembly] [indicated on Drawings].

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

          - Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - FIELD CONDITIONS

If possible, design railings so they do not have to fit other construction and delete this article.

        - Field Measurements: Verify actual locations of walls and other construction contiguous with railings by field measurements before fabrication and indicate measurements on Shop Drawings.

      - WARRANTY

When warranties are required, verify with Owner's counsel that warranties stated in this article are not less than remedies available to Owner under prevailing local laws.

"Manufacturer's Special Warranty for Laminated Glass" Paragraph below is an example only; revise to suit Project.

        - Manufacturer's Special Warranty for Laminated Glass: Glazed decorative metal railing manufacturer agrees to replace laminated-glass units that deteriorate within specified warranty period. Deterioration of laminated glass is defined as defects developed from normal use that are not attributed to glass breakage or to maintaining and cleaning laminated glass contrary to manufacturer's written instructions. Defects include edge separation, delamination materially obstructing vision through glass, and blemishes exceeding those allowed by referenced laminated-glass standard.

Verify available warranties and warranty periods. VIVA Railings recommends SGP as the interlayer material for laminated glass as it is structurally stronger, has better edge and laminate performance than PVB, and it has a five-year warranty. There is only a one-year warranty offered for the PVB interlayer material.

          - Warranty Period: [One] [Five] year[s] from date of Substantial Completion.

- PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

      - SOURCE LIMITATIONS

        - Obtain glazed decorative metal railing systems from single source from single manufacturer. Systems must be designed, engineered, and fabricated by manufacturer of railing system.

      - MANUFACTURERS

VIVA Railings, LLC, offers a full line of pre-engineered glazed decorative metal railing and guard systems as specified below. Many of the railing systems may be customized for curved applications, in addition to the standard straight modular applications. For a visual overview, see https://vivarailings.com/products/.

Railings and guards specified in this article are fabricated from laminated glass panels in the following configurations and profiles listed below. Coordinate with VIVA Railings.

SOLO: Top-, fascia-, or core-mounted to steel stringer or balcony slab edge with profiled single-flat bar posts with glass infill panels; steel posts are also available; see https://vivarailings.com/products/ornamental-stainless-steel-glass-railings-solo/ for product options.

        - Glazed Decorative Metal Railings:

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

          - Basis-of-Design Product: Subject to compliance with requirements, provide VIVA Railings, LLC; SOLO Railing System or comparable product by one of the following:

            - <Insert manufacturer's name>.

        - Illuminated Decorative Metal Railings:

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

          - Basis-of-Design Product: Subject to compliance with requirements, provide VIVA Railings, LLC; iRAIL [Linear] [Pods] Railing System or comparable product by one of the following:

            - <Insert manufacturer's name>.

        - Product Options: Drawings indicate size, profiles, and dimensional requirements of railings and are based on the specific system indicated. See Section 016000 "Product Requirements."

          - Do not modify intended aesthetic effects, as judged solely by Architect, except with Architect's approval. If modifications are proposed, submit comprehensive explanatory data to Architect for review.

      - PERFORMANCE REQUIREMENTS

        - General: For engineering glazed decorative metal railings to withstand structural loads indicated, determine allowable design working stresses of railing materials based on the following:

          - Stainless Steel: 45 percent of minimum yield strength.

          - Steel: 72 percent of minimum yield strength.

        - Structural Performance: Glazed decorative metal railings, including attachment to building construction, shall withstand the effects of gravity loads and the following loads and stresses within limits and under conditions indicated:

Three subparagraphs below are based on the IBC; revise to suit Project and to comply with requirements of authorities having jurisdiction.

          - Handrails[ and Top Rails of Guards]:

            - Uniform load of 50 lbf/ft. (0.73 kN/m) applied in any direction.

            - Concentrated load of 200 lbf (0.89 kN) applied in any direction.

            - Uniform and concentrated loads need not be assumed to act concurrently.

          - Glass Infill Panels:

            - Concentrated load of 50 lbf (0.22 kN) applied horizontally on an area of 1 sq. ft. (0.093 sq. m).

            - Infill load and other loads need not be assumed to act concurrently.

Retain "Wind Loads" Paragraph below for exterior glazed decorative metal railings; delete if only interior railings are required for Project.

        - Wind Loads: For exterior glazed decorative metal railings, capable of withstanding the following wind loads in accordance with the IBC and ASTM E1300:

          - Wind Load: [As indicated on Drawings] <Insert wind load>.

Retain "Windborne-Debris-Impact Resistance" Paragraph below for exterior glazed decorative metal railings in hurricane-prone areas. The IBC establishes criteria for buildings in hurricane-prone locations. In paragraph, "enhanced" option applies to essential facilities and has additional requirements. Verify requirements of authorities having jurisdiction. Verify which manufacturers have tested products and can demonstrate compliance.

        - Windborne-Debris-Impact Resistance: Exterior glazed decorative metal railings passing ASTM E1886 missile-impact and cyclic-pressure tests in accordance with ASTM E1996 for Wind Zone [1] [2] [3] [4] for [basic] [enhanced] protection.

Insert increased heights if different from those in "Large-Missile Test" and "Small-Missile Test" subparagraphs below. For enhanced protection, delete "Small-Missile Test" Subparagraph.

          - Large-Missile Test: For exterior glazing located within [30 ft. (9.1 m)] <Insert dimension> of grade.

          - Small-Missile Test: For exterior glazing located between 30 ft. (9.1 m) and [60 ft. (18.3 m)] <Insert dimension> above grade.

Delete "Thermal Movements" Paragraph below if only interior railings are required.

        - Thermal Movements: Allow for thermal movements from ambient and surface temperature changes acting on exterior railings by preventing buckling, opening of joints, overstressing of components, failure of connections, and other detrimental effects.

Differential values in "Temperature Change" Subparagraph below are suitable for most of the United States.

          - Temperature Change: 120 deg F (67 deg C), ambient; 180 deg F (100 deg C), material surfaces.

      - METALS, GENERAL

        - Metal Surfaces, General: Provide materials with smooth surfaces, without seam marks, roller marks, rolled trade names, stains, discolorations, or blemishes.

        - Brackets, Flanges, and Anchors: Same metal and finish as supported rails unless otherwise indicated.

          - Provide stainless steel wall brackets with flange tapped for concealed anchorage with vertical and horizontal adjustment capability.

      - STAINLESS STEEL

Retain "Recycled Content of Stainless Steel Products" Paragraph below to specify recycled content if required. An alternative method of requiring recycled content is to retain requirement in Project's Division 01 sustainable design requirements Section that gives Contractor the option and responsibility to determine how recycled content requirements will be met.

        - Recycled Content of Stainless Steel Products: Postconsumer recycled content plus one-half of preconsumer recycled content not less than 65 percent.

VIVA Railings' standards are Types 304 and 316. Type 316L is available upon special request and with additional cost for use on projects requiring better resistance to corrosion and exposure to de-icing salts. Coordinate material options with VIVA Railings.

Retain material types, qualities, and grades in this article that are indicated in the Specifications or on Drawings. Grade designations MT, TP, and CF below relate to the form of metal (tubing, pipe, or castings) being specified.

        - Tubing: ASTM A554, [Grade MT 304] [Grade MT 316].

Retain first option in "Castings" Paragraph below with Type 304; retain second option with Type 316.

        - Castings: ASTM A743/A743M, [Grade CF 8 or Grade CF 20] [Grade CF 8M or Grade CF 3M].

        - Sheet, Strip, Plate, and Flat Bar: ASTM A666 or ASTM A240/A240M, [Type 304] [Type 316].

        - Bars and Shapes: ASTM A276, [Type 304] [Type 316].

      - STEEL

        - Bars: Hot-rolled, carbon steel complying with ASTM A29/A29M, Grade 1010.

      - GLASS AND GLAZING PRODUCTS, GENERAL

Maximum glass panel widths vary from 4 ft. (1.219 m) to 5 ft. (1.524 m) in accordance with VIVA Railing System used. Coordinate with VIVA Railings.

See https://vivarailings.com/infill-systems-guide/glass-infills/ for additional information regarding available glass panel options.

        - Glazing Publications: Comply with written instructions of glass product manufacturers and organizations below unless more stringent requirements are indicated. See these publications for glazing terms not otherwise defined in this Section or in referenced standards.

Retain publications in "NGA/GANA Publications" Subparagraph below that apply to glass products specified.

          - NGA/GANA Publications: ["GANA Laminated Glazing Reference Manual" and ]"GANA Glazing Manual."

        - Safety Glazing: Glazing shall comply with 16 CFR 1201, Category II.

Retain "Safety Glazing Labeling" Paragraph below if applicable and if labeling is required. Not all manufacturers participate in third-party testing programs.

        - Safety Glazing Labeling: Permanently mark glass with certification label of [the SGCC] [the SGCC or another certification agency acceptable to authorities having jurisdiction] [or] [manufacturer]. Label shall indicate manufacturer's name, type of glass, thickness, and safety glazing standard with which glass complies.

Retain one or more of "Clear Annealed Float Glass," "Low-Iron Float Glass," "Tinted Annealed Float Glass," "Fully Tempered Float Glass," and "Heat-Strengthened Float Glass" paragraphs below for primary float glass types and classifications.

        - Clear Annealed Float Glass: ASTM C1036, Type I, Class 1 (clear), Quality-Q3.

        - Low-Iron Float Glass: ASTM C1036, Type I, Class I (clear), Quality-Q3; and with visible light transmission of not less than 91 percent.

        - Tinted Annealed Float Glass: ASTM C1036, Type I, Class 2 (tinted), Quality-Q3.

        - Fully Tempered Float Glass: ASTM C1048, Kind FT (fully tempered), Condition A (uncoated) unless otherwise indicated, Type I, Class 1 (clear), Class 1 and low-iron clear, or Class 2 (tinted) as indicated, Quality-Q3.

        - Heat-Strengthened Float Glass: ASTM C1048, Kind HS (heat strengthened), Type I, Condition A (uncoated) unless otherwise indicated, Type I, Class 1 (clear) or Class 2 (tinted) as indicated, Quality-Q3.

Retain one or more of "Ceramic-Coated Glass," "Tempered Patterned Glass," "Patterned Ultraclear Glass," "Tempered Patterned Ultraclear Glass," and "Decorative Film Overlay" paragraphs below for "decorative" glass types and classifications for VIVA Railings' Deco Glass infill options.

See https://vivarailings.com/finishing-options/glass-patterns/ for additional information and patterns.

        - Ceramic-Coated Glass: Heat-strengthened float glass, Condition C; with ceramic enamel applied by silk-screened process; complying with Specification No. 95-1-31 in GANA's "Engineering Standards Manual" and with other requirements specified.

          - Decorative Glass Pattern: <Insert Pattern No.>

        - Tempered Patterned Glass: ASTM C1048, Kind FT (fully tempered), Type II, Class 1 (clear) or Class 2 (tinted) as indicated, Form 3; finish, pattern, and quality as indicated.

          - Decorative Glass Pattern: <Insert Pattern No.>

        - Patterned Ultraclear Glass: ASTM C1036, Type II, Class 1 (clear), Form 3, with visible light transmission not less than 91 percent; finish, pattern, and quality as indicated.

          - Decorative Glass Pattern: <Insert Pattern No.>

        - Tempered Patterned Ultraclear Glass: ASTM C1048, Kind FT (fully tempered), Type II, Class 1 (clear), Form 3, with visible light transmission not less than 91 percent; finish, pattern, and quality as indicated.

          - Decorative Glass Pattern: <Insert Pattern No.>

        - Decorative Film Overlay: Translucent, dimensionally stable, cast PVC film, 2-mil- (0.05-mm-) minimum thickness, with pressure-sensitive, clear adhesive back for adhering to glass and releasable protective backing.

          - Decorative Film Pattern: <Insert Pattern No.>

        - Bent Glass: ASTM C1464, [Kind BFT (bent, tempered)] [Kind BHS, (bent, heat strengthened)] [Kind BL, (bent, laminated)].

      - GLASS INFILL PANELS

        - Tempered Glass: Provide products that have been tested for surface and edge compression in accordance with ASTM C1048 and for impact strength in accordance with 16 CFR 1201 for Category II materials.

          - Glass Color: [Clear] <Insert color>.

Retain one or more thickness requirements in "Thickness for Glass Infill Panels" and "Glass Thickness" subparagraphs below. Tinted glass is not available in thicknesses more than 0.47 inch (12 mm). Verify thickness by structural analysis. Verify, with railing manufacturers, availability of glass thicknesses. The IBC limits locations of non-laminated, single-pane (monolithic) tempered glass in handrails or guards.

          - Thickness for Glass Infill Panels: As required by structural loads, but not less than [0.39 inch (10 mm)] [0.51 inch (13 mm)].

          - Glass Thickness: As indicated on Drawings.

        - Laminated Glass: ASTM C1172, Type II with two plies of glass bonded together by an interlayer.

          - Construction: Laminate glass with interlayer.

          - Interlayer Thickness: [0.030 inch (0.76 mm)] [0.060 inch (1.52 mm)] [0.090 inch (2.29 mm)].

Retain one of first two options in "Kind" Subparagraph below or retain "As indicated" option and indicate kinds required in "Fabrication of Glass Infill Panels" Article.

          - Kind: [LT (laminated tempered)] [As indicated].

          - Glass Color: Inner-ply [clear] [low-iron clear] [blue] [blue-green] [bronze] [green] [gray] <Insert color>; outer-ply [clear] [low-iron clear] [blue] [blue-green] [bronze] [green] [gray] <Insert color>.

          - Ceramic Coating Color and Pattern: [As selected by Architect from manufacturer's full range] <Insert manufacturer's color and pattern designation>, applied to [inner] [outer] glass ply.

VIVA Railings recommends SGP as the interlayer material, as it is structurally stronger, has better edge and laminate performance than PVB, and it has a five-year warranty. There is only a one-year warranty for the PVB interlayer material.

Retain one of two "Interlayer" subparagraphs below.

          - Interlayer: SGP; [0.035 inch (0.89 mm)] [0.060 inch (1.52 mm)] thick.

            - Interlayer Color: [Clear] [Translucent White].

          - Interlayer: PVB; 0.060 inch (1.52 mm) thick.

            - Interlayer Color: [Clear] [Blue-green] [Bronze light] [Gray] <Insert color>.

Retain one or more thickness requirements in "Glass Plies for Glass Infill Panels" subparagraph below. Verify thickness by structural analysis. Verify, with railing manufacturers, availability of glass thicknesses.

          - Glass Plies for Glass Infill Panels: Thickness required by structural loads, but not less than [0.20 inch (5 mm)] [0.24 inch (6 mm)] thick each.

Retain "Windborne-Debris-Impact-Resistant Laminated Glass Guards" Paragraph below if retaining "Windborne-Debris-Impact Resistance" Paragraph in "Performance Requirements" Article.

        - Windborne-Debris-Impact-Resistant Laminated Glass Guards: ASTM C1172, Type II with two plies of glass bonded together with an interlayer.

          - Construction: Laminate glass with [polyvinyl butyral interlayer] [or] [ionoplast polymer interlayer] to comply with interlayer manufacturer's written instructions.

          - Interlayer Thickness: [0.060 inch (1.52 mm)] [0.090 inch (2.29 mm)].

Retain one of first two options in "Kind" Subparagraph below or retain "As indicated" option and indicate kinds required in "Fabrication of Glass-Infill Panels" Article.

          - Kind: [LHS (laminated heat strengthened)] [LT (laminated tempered)] [As indicated].

          - Glass Color: Inner-ply [clear] [low-iron clear] [blue] [blue-green] [bronze] [green] [gray] <Insert color>; outer-ply [clear] [low-iron clear] [blue] [blue-green] [bronze] [green] [gray] <Insert color>.

          - Ceramic Coating Color and Pattern: [As selected by Architect from manufacturer's full range] <Insert manufacturer's color and pattern designation>, applied to [inner] [outer] glass ply.

          - Interlayer Color: [Clear] [Blue-green] [Bronze light] [Gray] <Insert color>.

Retain "Interlayer Color and Pattern" Subparagraph below for interlayer with printed decorative pattern.

          - Interlayer Color and Pattern: [As selected by Architect from manufacturer's full range] [Match] [Provide] <Insert manufacturer's color and pattern designation>.

Retain one or more thickness requirements in "Glass Plies for Glass Infill Panels" subparagraph below. Verify thickness by structural analysis. Verify, with railing manufacturers, availability of glass thicknesses.

          - Glass Plies for Glass Infill Panels: Thickness required by structural loads, but not less than [4.0] [5.0] mm each.

        - Dry-Set Continuous Compression Mounting Accessories for Glass Infill Panels: As supplied by railing manufacturer for installing glass panels within railing system.

      - ILLUMINATED RAILINGS

Revise "General" Paragraph below if using another type of railing. Product below is VIVA Railings' standard. See https://vivarailings.com/products/led-illuminated-railing-system/ for product options.

VIVA Railings' iRAIL can be used as a Top Rail, Glass Top Cap, Assist Rail, Wall Rail, or FSR application.

        - General: Comply with requirements in this Section for metal railings with welded connections.

        - Illuminated Units: Provide internally wired [1-1/2-inch- (38-mm-) diameter stainless steel] [2-inch- (51-mm-) diameter stainless steel] [2-inch- (50-mm-) diameter wood] rail with integral LED light fixture system to illuminate walking surfaces adjacent to railings without light leaks. Make provisions for servicing and for concealed connection to electric service. Coordinate electrical characteristics with power supply provided.

          - Light Color: [Cool white; 4000 K] [Warm white; 3000 K].

          - IP Rating: IP67.

Retain next six subparagraphs below for iRail Linear illuminated rail system.

          - Light Output: [185 lumens/ft.] [250 lumens/ft.]

          - Beam Angle: 120 degrees.

          - Orientation: [Symmetrical] [Asymmetrical at 30 degrees].

          - LED Lens: [Clear] [Frosted].

          - CRI: Less than 90.

          - Power Supply: [120 V] [277 V] ac input, 12 V dc output.

Retain next six subparagraphs below for iRail Pods illuminated rail system.

          - Light Spacing: [18 inches (457 mm)] [36 inches (914 mm)] o.c.

          - Light Output: [90 lumens] [76 lumens].

          - Beam Angle: 60 degrees.

          - Orientation: [Symmetrical] [Asymmetrical at 22 degrees].

          - CRI: Less than 90.

          - Power Supply: [120 V] [277 V] ac input, 24 V dc output.

      - WOOD RAILINGS

Retain one of two "Description" paragraphs below. Retain first paragraph if wood rails are supplied by railing manufacturer; retain second paragraph if they are supplied by architectural woodworker in Division 06.

        - Description: Clear, straight-grained hardwood rails secured to [recessed] [exposed] metal substrate.

Other species in "Species" Subparagraph below are available upon request from VIVA Railings. All VIVA Railings' wood rails are shipped unfinished for field finishing under Section 099123 "Interior Painting." Standard shape and size is round, 2-inch (50-mm) diameter.

          - Species: [Cherry] [Maple] [Red oak] [White oak] <Insert species>.

          - Finish: Manufacturer's standard, unfinished.

          - Staining: In accordance with Section 099123 "Interior Painting."

If rails are required to serve as handrails rather than only as top rails of guards, verify that profile specified will comply with applicable regulations for accessibility to people with disabilities.

          - Profile: [Square, 1-3/4 by 1-3/4 inches (45 by 45 mm) with edges eased to 1/4-inch (6-mm) radius] [Rectangular, 1-3/4 by 5 inches (45 by 127 mm) with edges eased to 1/4-inch (6-mm) radius] [Round, 2-inch (50-mm) diameter] [As indicated] <Insert description>.

          - Handrail Profile: [Round, 2-inch (50-mm) diameter] [Round, 1-1/2-inch (38-mm) diameter, reinforced] [Rectangular, 1-1/4 by 1-3/4 inches (32 by 45 mm) with edges eased to 1/4-inch (6-mm) radius] [As indicated] <Insert description>.

First "Certified Wood" Subparagraph below applies to LEED 2009 and LEED v4. Manufacturers certifying products as "FSC Mixed Credit" do not have to use 100 percent certified wood in the products; however, in their total production, manufacturers must use an amount equal to or greater than the percentage of their production that is labeled "FSC Mixed Credit."

          - Certified Wood: Wood products shall be certified as "FSC Pure"[ or "FSC Mixed Credit"] in accordance with FSC STD-01-001 and FSC STD-40-004.

"Certified Wood" Subparagraph below applies to IgCC.

          - Certified Wood: Wood products shall be labeled in accordance with the AF&PA's Sustainable Forestry Initiative, be certified as "FSC Pure" in accordance with FSC STD-01-001 and FSC STD-40-004, or be certified and labeled in accordance with the standards of the Programme for Endorsement of Forest Certification.

"Certified Wood" Subparagraph below applies to ASHRAE 189.1.

          - Certified Wood: Wood products shall [contain not less than 60 percent] [be made from] certified wood tracked through a chain-of-custody process. Certified wood documentation shall be provided by sources certified through a forest certification system with principles, criteria, and standards developed using ISO/IEC Guide 59 or the World Trade Organization's "WTO Agreement on Technical Barriers to Trade."

"Certified Wood" Subparagraph below applies to Green Globes.

          - Certified Wood: Wood products shall be certified in accordance with the American Tree Farm System's "AFF Standard," the AF&PA's Sustainable Forestry Initiative, FSC STD-01-001 and FSC STD-40-004, or the standards of the Programme for Endorsement of Forest Certification.

        - Description: Hardwood rails complying with Section 064023 "Interior Architectural Woodwork."

      - FASTENERS

        - Fastener Materials: Unless otherwise indicated, provide the following:

          - For Stainless Steel Components: [Type 304] [Type 316] stainless steel fasteners.

          - For Dissimilar Metals: [Type 304] [Type 316] stainless steel fasteners.

Retain subparagraph below if exposed fasteners are allowed.

          - Finish exposed fasteners to match appearance, including color and texture, of railings.

        - Fasteners for Anchoring to Other Construction: Select fasteners of type, grade, and class required to produce connections suitable for anchoring railings to other types of construction indicated[ and capable of withstanding design loads].

        - Provide concealed fasteners for interconnecting railing components and for attaching railings to other work unless [otherwise indicated] [exposed fasteners are unavoidable] [exposed fasteners are the standard fastening method for railings indicated].

Revise subparagraph below if another type of head is required or is standard with system specified.

          - Provide hex, hex socket, or hex button machine screws for exposed fasteners unless otherwise indicated.

ICC-ES AC193 is for mechanical anchors; ICC-ES AC308 is for adhesive anchors.

        - Post-Installed Anchors: Fastener systems with working capacity greater than or equal to design load, in accordance with an evaluation report acceptable to authorities having jurisdiction, based on ICC-ES AC193[ or ICC-ES AC308].

Material in "Material for Interior Locations" Subparagraph below protects against corrosion in an indoor atmosphere.

          - Material for Interior Locations: Carbon-steel components zinc plated to comply with ASTM B633 or ASTM F1941/ASTM F1941M, Class Fe/Zn 5, unless otherwise indicated.

First option in "Material for Exterior Locations and Where Stainless Steel Is Indicated" Subparagraph below refers to Type 304 and similar alloys; second option refers to Type 316 and similar alloys.

          - Material for Exterior Locations and Where Stainless Steel Is Indicated: Alloy [Group 1 (A1)] [Group 2 (A4)] stainless steel bolts, ASTM F593, and nuts; ASTM F594 (ASTM F836M).

      - MISCELLANEOUS MATERIALS

        - Handrail Brackets: Stainless steel with center of rail [2-1/2 inches (63.5 mm)] [3-1/8 inches (79.4 mm)] <Insert dimension> from face of structural glass balusters.

Usually retain one of three subparagraphs below that corresponds with type of bracket used. Delete all three if wall rails are not used.

          - Provide brackets with flange tapped for concealed anchorage to threaded hanger bolt.

          - Provide brackets with predrilled hole for exposed bolt anchorage.

          - Provide brackets with predrilled hole for bolted anchorage and with snap-on cover that matches rail finish and conceals bracket base and bolt head.

Retain "Nonshrink, Nonmetallic Grout" or "Anchoring Cement" Paragraph below, or both, to suit Project.

        - Nonshrink, Nonmetallic Grout: Factory-packaged, nonstaining, noncorrosive, nongaseous grout complying with ASTM C1107/C1107M. Provide grout specifically recommended by manufacturer for [interior] [and] [exterior] applications.

        - Anchoring Cement: Factory-packaged, nonshrink, nonstaining, hydraulic-controlled expansion cement formulation for mixing with water at Project site to create pourable anchoring, patching, and grouting compound.

          - Water-Resistant Anchoring Cement: [At exterior locations] [and] [where indicated] provide formulation that is recommended in writing to be resistant to erosion from water exposure without needing protection by a sealer or waterproof coating.

      - FABRICATION

        - General: Fabricate glazed decorative metal railings to comply with requirements indicated for design, dimensions, member sizes and spacing, details, finish, and anchorage[, but not less than that required to support structural loads].

        - Shop assemble railings and guards to greatest extent possible to minimize field splicing and assembly. Disassemble units only as necessary for shipping and handling limitations. Clearly mark units for reassembly and coordinated installation. Use connections that maintain structural value of joined pieces.

        - Cut, drill, and punch metals cleanly and accurately. Remove burrs and ease edges to a radius of approximately 1/32 inch (1 mm) unless otherwise indicated. Remove sharp or rough areas on exposed surfaces.

        - Form work true to line and level with accurate angles and surfaces.

        - Fabricate connections that will be exposed to weather in a manner to exclude water. Provide weep holes where water may accumulate. Locate weep holes in inconspicuous locations.

        - Cut, reinforce, drill, and tap as indicated to receive finish hardware, screws, and similar items.

        - Mechanical Connections: Connect members with concealed mechanical fasteners and fittings. Fabricate members and fittings to produce flush, smooth, rigid, hairline joints.

          - Fabricate splice joints for field connection using an epoxy structural adhesive if this is manufacturer's standard splicing method.

        - Form changes in direction as follows:

Retain one of five subparagraphs below. Second subparagraph allows fabricator to choose radius of bends. Third is for flush (zero-radius) bends. Fourth is for radii that are indicated on Drawings.

          - As detailed.

          - [By bending] [or] [by inserting prefabricated elbow fittings].

          - [By flush bends] [or] [by inserting prefabricated flush-elbow fittings].

          - [By radius bends of radius indicated] [or] [by inserting prefabricated elbow fittings of radius indicated].

          - By bending to smallest radius that will not result in distortion of railing member.

Retain first paragraph below if bending is allowed or required.

        - Bend members in jigs to produce uniform curvature for each configuration required; maintain cross section of member throughout entire bend without buckling, twisting, cracking, or otherwise deforming exposed surfaces of components.

        - Close exposed ends of hollow railing members with prefabricated cap and end fittings of same metal and finish as railings.

        - Brackets, Flanges, Fittings, and Anchors: Provide wall brackets, flanges, handrail brackets, miscellaneous fittings, and anchors to interconnect railing members to other Work unless otherwise indicated.

Retain subparagraph below if any railings are supported from plaster or gypsum board walls.

          - At brackets and fittings fastened to plaster or gypsum board partitions, provide crush-resistant fillers, or other means to transfer loads through wall finishes to structural supports and to prevent bracket or fitting rotation and crushing of substrate.

        - Provide inserts and other anchorage devices for connecting railings to concrete or masonry work. Fabricate anchorage devices capable of withstanding loads imposed by railings. Coordinate anchorage devices with supporting structure.

Delete paragraph below if no posts are set in concrete or if posts are set without sleeves.

        - For railing posts set in concrete, provide [steel] [stainless steel] sleeves not less than 6 inches (150 mm) long with inside dimensions not less than 1/2 inch (13 mm) greater than outside dimensions of post, with metal plate forming bottom closure.

      - FABRICATION OF GLASS INFILL PANELS

        - Fabricate glass to sizes and shapes required; provide for proper edge clearance and bite on glazing panels.

        - Glass Infill Panels: Provide [tempered] [laminated, heat-strengthened] [laminated, tempered] glass infill panels[ for both straight and curved sections].

Revise edging descriptions in "Edge Finish" Subparagraph below to suit Project.

          - Edge Finish: [Clean-cut or flat-grind edges to produce smooth, square edges with slight chamfers at junctions of edges and faces] <Insert edge finishes>.

      - METAL FINISH REQUIREMENTS, GENERAL

        - Comply with NAAMM's "Metal Finishes Manual for Architectural and Metal Products" recommendations for applying and designating finishes.

        - Protect mechanical finishes on exposed surfaces from damage by applying a strippable, temporary protective covering before shipment.

        - Appearance of Finished Work: Noticeable variations in same piece are not acceptable. Variations in appearance of abutting or adjacent pieces are acceptable if they are within one-half of the range of approved Samples. Variations in appearance of other components are acceptable if they are within the range of approved Samples and are assembled or installed to minimize contrast.

Retain paragraph below if exposed fasteners are allowed.

        - Provide exposed fasteners with finish matching appearance, including color and texture, of railings.

      - STAINLESS STEEL FINISHES

        - Surface Preparation: Remove tool and die marks and stretch lines, or blend into finish.

        - Stainless Steel Finishes:

Retain "Color Electro-Plated Metal" Subparagraph to suit Project.

          - Color Electro-Plated Metal: Vertical and stand-off components.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

            - Basis-of-Design Product: Subject to compliance with requirements, provide VIVA Railings, LLC; ECM Finish System or comparable product.

            - Color: Satin [Black (ECM-20)] [Gold (ECM-21)] [Brass (ECM-23)] [Copper (ECM-25)].

Finish in "Dull Satin Finish" Subparagraph below is a nondirectional finish produced from a No. 4 finish by brushing with a 380-grit extremely fine abrasive to remove the grit lines without producing a reflective appearance.

          - Dull Satin Finish: ASTM A480/A480M, No. 6.

      - STEEL FINISHES

        - Surface Preparation: Remove tool and die marks and stretch lines, or blend into finish.

        - Powder-Coat Finish: AAMA 2603 except with a minimum dry film thickness of 1.5 mils (0.04 mm). Comply with coating manufacturer's written instructions for cleaning, conversion coating, and applying and baking finish.

          - Color and Gloss: [As indicated by manufacturer's designations] [Match Architect's sample] [As selected by Architect from manufacturer's full range] <Insert color and gloss>.

- EXECUTION

      - EXAMINATION

Delete first paragraph below if no handrails are attached to plaster or gypsum board assemblies.

        - Examine plaster and gypsum board assemblies, where reinforced to receive anchors, to verify that locations of concealed reinforcements have been clearly marked for Installer. Locate reinforcements and mark locations if not already done.

        - Installation Tolerances: Structural steel and concrete slabs to be within 1/8 inch (3 mm) in 10 ft. (3.048 m) horizontally and 1/8 inch (3 mm) vertically. Correct out-of-tolerance conditions to meet railing manufacturer's requirements.

      - INSTALLATION, GENERAL

        - Comply with Drawings and manufacturer's written instructions for installing glazed decorative metal railings, accessories, and other components.

Retain "Windborne-Debris Resistance" Paragraph below for exterior installations requiring windborne-debris resistance. Proper anchorage of railings is necessary to maintain performance as tested.

        - Windborne-Debris Resistance: Anchor glazed decorative metal railings to structure using anchoring method, fastener type, and fastening frequency identical to that used in windborne-debris-resistance testing.

        - Perform cutting, drilling, and fitting required for installing metal railings.

          - Fit exposed connections together to form tight, hairline joints.

          - Install railings level, plumb, square, true to line; without distortion, warp, or rack.

          - Set railings accurately in location, alignment, and elevation; measured from established lines and levels.

          - Do not weld, cut, or abrade surfaces of metal railing components that have been coated or finished after fabrication and that are intended for field connection by mechanical or other means without further cutting or fitting.

Revise two subparagraphs below if closer tolerances are required. Both are from NAAMM's "Pipe Railing Systems Manual."

          - Set posts plumb within a tolerance of 1/16 inch in 3 ft. (2 mm in 1 m).

          - Align rails so variations from level for horizontal members and variations from parallel with rake of steps and ramps for sloping members do not exceed 1/4 inch in 12 ft. (5 mm in 3 m).

        - Control of Corrosion: Prevent galvanic action and other forms of corrosion by insulating metals and other materials from direct contact with incompatible materials.

        - Adjust railings before anchoring to ensure matching alignment at abutting joints.

        - Fastening to In-Place Construction: Use anchorage devices and fasteners where necessary for securing railings and for properly transferring loads to in-place construction.

      - METAL RAILING CONNECTIONS

        - Nonwelded Connections:

          - Use mechanical or adhesive joints for permanently connecting railing components.

          - Use wood blocks and padding to prevent damage to railing members and fittings.

          - Seal recessed holes of exposed locking screws using plastic cement filler colored to match finish of railings.

Retain "Expansion Joints" Paragraph below if expansion joints are required or revise to suit Project. Indicate locations on Drawings based on temperature changes expected and coefficient of expansion of metals involved.

        - Expansion Joints: Install expansion joints at locations indicated, but not farther apart than required to accommodate thermal movement. Provide slip-joint internal sleeve extending 2 inches (50 mm) beyond joint on either side, fasten internal sleeve securely to one side, and locate joint within 6 inches (150 mm) of post.

      - ANCHORING METAL POSTS

Retain type(s) of anchorage in this article to suit Project.

Retain one of first two paragraphs below, or delete both if no posts in concrete. Coordinate with products specified in Part 2.

        - Use stainless steel pipe sleeves preset and anchored into concrete for installing posts. After posts have been inserted in sleeves, fill annular space between post and sleeve with [nonshrink, nonmetallic grout] [or] [anchoring cement], mixed and placed to comply with anchoring material manufacturer's written instructions.

        - Form or core-drill holes in accordance with engineering requirements for installing posts in concrete. Clean holes of loose material, insert posts, and fill annular space between post and concrete with [nonshrink, nonmetallic grout] [or] [anchoring cement], mixed and placed to comply with anchoring material manufacturer's written instructions.

Retain one of first two paragraphs below if retaining either concrete anchorage method above.

        - Cover anchorage joint with flange of same metal as post, [welded to post after placing anchoring material] [attached to post with setscrews].

        - Leave anchorage joint exposed with [1/8-inch (3-mm) buildup, sloped away from post] [anchoring material flush with adjacent surface].

Revise first paragraph below if posts are welded directly to supports.

        - Anchor posts to metal surfaces with flanges, angle type, or floor type as required by conditions, connected to posts and to metal supporting members as follows:

Retain one of two subparagraphs below.

          - For stainless steel railings, weld flanges to posts and bolt to metal-supporting surfaces.

          - For steel railings, weld flanges to posts and bolt to metal-supporting surfaces.

Retain paragraph below if applicable.

        - Install removable railing sections, where indicated, in slip-fit metal sockets cast in concrete.

For post-supported railings and guards with glass infill panels, retain Article below and requirements in other Part 3 articles that apply to type of railing construction used.

      - INSTALLATION OF GLASS INFILL PANELS

        - Post-Supported Railings and Guards with Glass Infill Panels:

          - Install assembly to comply with railing manufacturer's written instructions and with requirements in other Part 3 articles.

          - Erect posts and other metal railing components, and set factory-cut glass infill panels.

          - Do not cut, drill, or alter glass infill panels in field. Protect edges from damage.

      - FIELD QUALITY CONTROL

Retain this article if field testing for compliance with performance requirements is required in addition to product test reports and preconstruction testing.

        - Testing Agency: Owner will engage a qualified testing agency to perform tests and inspections and to prepare test reports. Payment for these services will be made [by Owner] [from the testing and inspecting allowance, as authorized by Change Orders].

Revise "Extent and Testing Methodology" Paragraph below if more extensive testing is required.

        - Extent and Testing Methodology: Testing agency will randomly select completed railing assemblies for testing that are representative of different railing designs and conditions in the completed Work. Test railings in accordance with ASTM E894, ASTM E935, ASTM E2353, and ASTM E2358 for compliance with performance requirements.

        - Remove and replace railings where test results indicate that they do not comply with specified requirements unless they can be repaired in a manner satisfactory to Architect and comply with specified requirements.

        - Perform additional testing and inspecting, at Contractor's expense, to determine compliance of replaced or additional work with specified requirements.

      - CLEANING

        - Clean decorative metal finishes by washing thoroughly with water and soap, rinsing with clean water, and wiping dry.

        - Clean and polish glass as recommended in writing by manufacturer. Wash both exposed surfaces in each area of Project not more than four days before date scheduled for inspections that establish date of Substantial Completion.

        - Clean wood rails by wiping with a damp cloth and then wiping dry.

      - PROTECTION

Maintain railing system with monthly washing with soap and water. This is particularly critical in salt environments or conditions to prevent corrosion.

        - Protect finishes of railings from damage during construction period with temporary protective coverings approved by railing manufacturer. Remove protective coverings at time of Substantial Completion.

        - Restore finishes damaged during installation and construction period so no evidence remains of correction work. Return items that cannot be refinished in the field to the shop; make required alterations and refinish entire unit, or provide new units.

END OF SECTION 057313