| METALSPACES — WALLSCAPES | SECTION 32 31 19 | DECORATIVE METAL FENCE & LANDSCAPE SCREENS |
| --- | --- | --- |

Edit bracketed [ ] items to match project requirements. Delete unused options.

PART 1 — GENERAL

1.1  SUMMARY

A. Section Includes:

- Decorative laser-cut metal panel fences and landscape screens.

- Exterior laser-cut metal wall panels and screens.

- FotoFacade image-perforated metal panels.

- Fasteners and miscellaneous attachment hardware.

B. Related Sections:

- 03 30 00 — Cast-in-Place Concrete (mounting substrate)

- 04 20 00 — Unit Masonry (mounting substrate)

- 05 12 00 — Structural Steel Framing (mounting substrate)

- 06 10 53 — Miscellaneous Rough Carpentry (wood blocking for anchoring)

1.2  DEFINITIONS

- WallScapes Decorative Metal Panel System: Laser-cut metal panels used as fences, landscape screens, and exterior wall screens providing pedestrian guidance, visual separation, HVAC/equipment screening, and architectural expression.

- FotoFacade: Custom image-perforated metal panel system; image file furnished by Architect/Designer.

1.3  PERFORMANCE REQUIREMENTS

A. Structural:

- Panels and attachments shall resist gravity, live, and wind loads as indicated on Drawings.

- Design Wind Loads: Per project Drawings. (Delete if interior-only.)

B. Thermal Movement (Exterior):

- Ambient temperature change: 120°F (67°C).

- Material surface temperature change: 180°F (100°C).

- Accommodate movement without buckling, joint opening, or connection failure.

C. Fire:

- Exterior assemblies: Comply with NFPA 285 where required by code.

1.4  SUBMITTALS

A. Product Data:

- Manufacturer's standard panel product data, materials, finishes, and available patterns.

- Fasteners, brackets, and bituminous paint.

B. Sustainable Design (if applicable):

- Recycled content documentation: postconsumer and preconsumer percentages and cost.

1.5  QUALITY ASSURANCE

A. Installer:

- Minimum 3 years experience installing comparable decorative metal panel systems.

B. Welding:

- Qualify procedures and personnel per applicable AWS code:

  - Steel: AWS D1.1/D1.1M

  - Aluminum: AWS D1.2/D1.2M

  - Stainless Steel: AWS D1.6/D1.6M

1.6  COORDINATION

- Furnish setting drawings, templates, and directions for embedded anchors (sleeves, inserts, anchor bolts) in time for substrate construction.

- Where panels screen electrical transformers, coordinate grounding with owner or equipment supplier per NEMA 250.

- Verify field dimensions before fabrication; note on Shop Drawings.

- Schedule installation so attachments coordinate with other trades. Do not temporarily support panels in any manner that does not meet structural performance requirements.

PART 2 — PRODUCTS

2.1  MANUFACTURERS

- Basis of Design: VIVA Railings / MetalSpaces — WallScapes Landscape and Fence System.

- Contact: info@vivarailings.com | virarailings.com/products/wall-systems

- Substitutions: Not permitted.

- Source Limitation: Obtain all panels, components, and hardware from single manufacturer.

2.2  MATERIALS

- Aluminum: ASTM B209, Alloy 5052-H32 — 1/8", 3/16", or 1/4" as required for design loads.

- Stainless Steel: ASTM A666, Type 304 — 14 Ga.

- Steel: ASTM A1008/A1008M, Type B — 14 Ga standard; 11 Ga where indicated on Drawings.

2.3  PANELS AND PATTERNS

- Select from WallScapes full pattern library: Primary, Geometric, or Organic series; custom laser-cut; or FotoFacade. Reference MetalSpaces Pattern Data at virarailings.com/products/architectural-panels.

- Custom pattern: Design by Architect/Designer.

- FotoFacade image panels: Custom design; image file furnished by Architect/Designer.

- Standard patterns may be scaled open or closed provided structural integrity is maintained.

- Surfaces shall be smooth, free of seam marks, roller marks, stains, or blemishes.

2.4  FINISHES

A. Aluminum Finishes:

- Powder Coat — AAMA 2604: Super durable, high-impact. Color: [As selected by Architect].

- High Performance (PVDF) — AAMA 2605: ≥70% PVDF resin. Color: [As selected by Architect]. For coastal/severe environments.

- Mill Finish: Where indicated.

B. Stainless Steel Finishes:

- Brushed Satin

C. Steel Finishes:

- Zinc-rich primer + Powder Coat, AAMA 2604. Color: [As selected by Architect].

- Mill Finish

D. General:

- Comply with NAAMM Metal Finishes Manual for application and designation.

- Apply strippable protective film to finished surfaces before shipment.

- Noticeable finish variation within a single piece is not acceptable.

2.5  ATTACHMENTS AND HARDWARE

- Brackets, outriggers, post and support arms: Manufacturer's standard for system type and design loads. Steel finish: [Zinc-rich primer + powder coat AAMA 2604 / Galvanized / Primer coat].

- Aluminum sub-framing: Clear anodized or painted to match panels.

2.6  FASTENERS

- Stainless steel and aluminum components: Type 304 SS fasteners.

- Dissimilar metal connections: Type 304 SS fasteners.

- Exposed fastener heads: Match panel color via plastic cap or factory coating.

- Head type: Hex, hex socket, or hex-button machine screw.

- Anchors to structure: Type and grade as required for design loads and substrate.

2.7  MISCELLANEOUS MATERIALS

- Welding Electrodes: AWS specification matching base metal alloy; color-match and compatibility required.

- Bituminous Paint (isolation): ASTM D1187/D1187M, cold-applied asphalt emulsion. Apply at dissimilar metal contact points.

2.8  FABRICATION

A. General:

- Fabricate to design dimensions, member sizes, spacing, finish, and anchorage requirements.

- Shop-assemble to maximum extent possible; disassemble only as required for shipping.

- Mark units for reassembly and coordinated installation.

B. Workmanship:

- Cut, drill, and punch cleanly. Remove burrs and sharp edges from exposed surfaces.

- Form work true to line and level with accurate angles.

- Maintain member cross-section through bends — no buckling, twisting, or cracking.

C. Connections:

- Mechanical connections standard. Welded connections where indicated on Drawings.

- Welded joints: cope for close fit; finish exposed welds to NOMMA Joint Finish Standard No. 1 (ornamental quality — no evidence of weld).

- Brackets and anchors: Sized for structural loads; provide crush-resistant fillers at gypsum board partitions where applicable.

PART 3 — EXECUTION

3.1  EXAMINATION

- Verify substrate is plumb, level, and within tolerance before installation.

- Installation Tolerance: Substrate within 1/8" in 10 ft. horizontally and 1/8" vertically.

- Correct out-of-tolerance conditions before proceeding.

- Confirm locations of concealed reinforcements in gypsum assemblies before drilling.

3.2  INSTALLATION

A. General:

- Perform all cutting, drilling, and fitting required for installation.

- Install panels level, plumb, square, true to line — no distortion, warp, or rack.

- Align abutting joints before final anchoring.

- Do not cut, weld, or abrade factory-finished surfaces intended for mechanical connection in the field.

B. Corrosion Control:

- Prevent galvanic action by isolating dissimilar metals with bituminous paint or non-conductive isolators.

C. Connections:

- Mechanical (standard): Tighten fasteners per manufacturer's torque requirements.

- Welded (where indicated): Comply with fabrication welding requirements; AWS code qualified procedures.

3.3  PROTECTION AND MAINTENANCE

- Restore finishes damaged during construction so no evidence of repair remains.

- Return items that cannot be field-refinished to shop for complete refinishing or replacement.

- Ongoing Maintenance: Wash with soap and water monthly — critical in salt or coastal environments.

END OF SECTION 32 31 19